DOI: 10.1002/ ((please add manuscript number))

Article type: Full paper

Understanding the Meniscus-Guided Coating Parameters in Organic Field-Effect-Transistor Fabrications

Ming Chen, Boyu Peng, Shuyun Huang and Paddy Kwok Leung Chan*

M. Chen, Dr. B. Peng, S. Huang, Prof. P. K. L. Chan

Department of Mechanical Engineering

The University of Hong Kong

Pok Fu Lam Road, Hong Kong, China

E-mail: pklc@hku.hk

Keywords: crystal growth, blade coating, semiconductor morphology, organic transistors

Abstract

Meniscus-guided coating (MGC) is a widely studied method for achieving single-crystalline organic thin films and high-performance organic field-effect-transistors (OFETs). MGC method is mainly applicable on the soluble organic semiconductors with strong - overlap, and able to crystallize into thin films after the evaporation of solvents. In this work, four elementary factors including shearing speed (v), solute concentration (c), deposition temperature (T) and solvent boiling point (Tb) are unified to analyze crystal growth behavior in the meniscus-guided coating. By carefully varying and studying these four key factors, we confirm that v is the thickness regulation factor while c is proportional to crystal growth rate. The MGC crystal growth rate is also correlated to latent heat (L) of solvents and deposition temperature in an Arrhenius form. The latent heat of solvents is proportional to Tb. The OFET channels grown by the optimized MGC parameters show uniform crystal morphology (Rq < 0.25 nm) with decent carrier mobilities (average μ = 5.88 cm2 V-1 s-1 and highest μ = 7.68 cm2 V-1 s-1). Our studies provide a generalized formula to estimate the effects of these fabrication parameters which can serve as the crystal growth guidelines for the MGC approach. It is also an important cornerstone towards scaling up the OFETs for the sophisticated organic circuits or mass production.

- Introduction

Organic semiconductor thin films serve as critical layers in organic field-effect-transistors (OFETs), which determines the performance of the OFETs. Motivated by diverse OFET applications in functional electronics, such as memory devices, integrated circuits, sensors and etc., comprehensive studies of organic thin films are indispensable toward the high-performance OFETs for commercial applications.[1-6] As a low-cost and fast organic thin film fabrication method, solution processable meniscus-guided coating (MGC) has attracted tremendous attention and achieved impressive progresses on different OFET properties in recent years.[7-11] By combining the large area processing with high resolution lithography technique, more sophisticated circuits can also be realized by the integrations of OFETs. To date, the uniformity of the organic active layer in the OFETs is still a major bottleneck in scaling up the OFET fabrication. Recently, some MGC grown high quality organic crystals up to wafer scale have been demonstrated, which is believed to be able to advance the pace of the OFET development.[5,12,13] A specific investigation of how each processing parameter synchronizes with the others can provide valuable information in designing the fabrication setup.

MGC technique relies on meniscus line formation when the solution comes in contact with the substrate, forming the substrate-air, solvent-air and substrate-solvent interfaces. Crystallization of the organic molecules occurs at the substrate-solvent-air contact line while the substrate moves and the solvent evaporates. Currently, different MGC methods for organic semiconductor thin films deposition, such as dip coating, zone casting and blade coating and others,[2,5,7-17] have been demonstrated. Recent advances on the MGC crystallization mechanisms mainly depend on the surface energy (γ) analysis of the system. Zhang et al. observed a better molecular packaging in the poly(diketopyrrolopyrrole-thiophene-thieno[3,2,b]thiophene-thiophene) (DPP2T-TTT) thin film when the system surface energy decreased.[18] Similar results of surface energy regulation have been perceived by Vladimirov and co-workers. They observed n-type crystals could start to grow at the solvent-air interface if the surface energy of solvents was higher than that of crystals.[19] Other than the experimental parameters, physical modelling has also been employed to investigate the crystallization process of the thin films. In the classical model developed by LaMer et al., it was proposed that nucleation and the crystal growth were very sensitive to the solute concentration and the crystal growth only happened at the metastable state.[20] Similar observations have been confirmed by the fullerene nanowire grown on silicon dioxide and 3,9-bis(4-ethylphenyl)-peri-xanthenoxanthene (C2Ph-PXX) thin film grown on the pre-patterned silicon.[21,22] Actually, the MGC methods involve different associated processing parameters which would alter the quality of the deposited films. Currently, the exact correlations between these parameters are still not completely understood by the research community and an in-depth investigation of their correlations is highly desired.

In the current work, we systematically investigate and unify the influence of the four elementary factors, (i) shearing speed (v), (ii) solute concentration (c), (iii) deposition temperature (T) and (iv) boiling points of solvent (Tb), on the MGC crystal growth. The MGC method and the semiconductor we utilized are the blade coating and 2,7-dioctyl[1]benzothieno[3,2-b][1]benzothiophene (C8-BTBT), respectively. Under a certain deposition rate (dm/dt), we confirm that v serves as thickness regulation factor while c is directly proportional to the crystal growth rate. Moreover, the crystal growth undergoes a T dependent thermodynamic process with the energy barrier proportional to Tb. By carefully varying these four parameters, three distinct morphologies of the organic thin films can be observed. Type I has rough crystal surface while Type III shows negligible crystal growth on the substrate. Only Type II samples show uniform and smooth morphology with roughness (Rq) around 0.25 nm. The Type II OFETs show a promising average mobility (μ) of 5.88 cm2 V-1 s-1, about 9-fold of Type I’s value. We also provide a generalized governing equation which can correlate the thin film deposition rate with four processing variables. This growth process guideline can help us to understand the gap between the beginning of nucleation seeds and the final morphology of the organic thin films. The theoretical analysis allows us to adjust the experimental parameters in order to achieve a uniform organic active layer over a large area, which is crucial for the mass production and advanced OFET circuits or other organic electronics.

2. Results and Discussion

Organic crystal thin films were deposited by the temperature controlled blade coating technique (Figure 1).[23] In the current study, C8-BTBT, widely used for solution processable OFETs for its high solubility and high mobility was chosen for the semiconductor active layer material.[8,12,16,17,24,25] Expect for high mobility of the material itself, the coherent (band-like) transport behavior entitles C8-BTBT an incredible material for recently impactful physical studies via Hall effect, including accurate mobility extraction and identification of the role of grain boundaries.[26,27] Eight commonly used solvents (including dichloromethane (DCM), chloroform, heptane, toluene, chlorobenzene (CB), m-xylene, mesitylene and 1,2,3,4-Tetrahydronaphthalene (tetralin)) with different Tb and γ are used in the solution processing. The corresponding Tb and γ values are listed in Table 1.[28,29] We paid particular attention to the surface tension difference between substrate and solvent as it will determine the formation of the meniscus-line and level of supersaturation and thus crystal growth.[30] As shown in Figure S1, the γ of phenyltrichlorosilane (PTS) treated substrate is 43.35 mN m-1 and it is higher than all the solvents being used (Table 1). It suggests that these eight solvents are suitable for the solution shearing application. When the C8-BTBT solution was injected into the controlled gap between the blade and substrate (as shown in Figure 1), the higher surface tension of substrate would allow the solution to wet the surface, forming a low contact angle meniscus surface. While the solvents were evaporating under elevated temperatures along the meniscus, the organic molecules condensed to supersaturation at the solvent-air interface and solidified. As a result, the crystal thin films would deposit gradually with the movement of substrate following the nucleated seeds formed at the initial contact line.

The formation of the organic thin film actually involves a number of different parameters and here we pay particular attention on the v, c, T and Tb. Among them, v and c are correlated to the conservation of mass described in Equation (1), [23,31]

dmdt=ρoscavtosc=cd∀dt                                                                                                            (1)

where dm/dt is the mass transfer rate, ρosc is the density of organic semiconductor C8-BTBT (1133 kg m-3),[32] a is the width of the substrate, tosc is the apparent thickness of the organic semiconductor and d/dt is the instant solvent evaporation rate. It is important to mention that Equation (1) is only valid in the evaporation region as discussed in Ref. 31. At this regime, semiconductor molecules are deposited near the contact line due to the solvent evaporation as shown in Figure 1b. As shown in Equation (1), c is directly proportional to mass transfer rate if d/dt is a constant. On the other hand, v and tosc are inversely proportional and therefore the shearing speed has been utilized as the thickness regulation factor, which have been observed by other search groups.[31,33,34] In order to determine the exact correlation between v and tosc in a certain range of dm/dt, the same value of d/dt is required and it is actually a function of T and Tb as we will discuss later.

To explore the effects of T and Tb on crystal growth experimentally, a series of blade coating based on the solvents with different Tb and at different temperatures are performed. For a fair and reasonable comparison, v and c are kept constant. Since the solubility limit of the C8-BTBT would vary in different solvents, a relatively low concentration of 1 mg mL-1 was adopted for all the experiments to ensure all the cases are below the solubility limit.[8,17]  For the shearing speed, v, a moderate speed for the MGC technique, 100 μm s-1, was used.[12,35,36] The polarized optical microscope (POM) images of the deposited C8-BTBT thin films under different T and Tb are compared in Figure 2. The horizontal and vertical directions represent the increases of Tb and T, respectively. Three distinct types of morphologies can be observed. Type I has rough surface with significant crystal aggregations due to the rapid evaporation of solvents and high homogeneous nucleation rate. Rapid evaporation would lead to significant increase in the solute concentration at the meniscus which favors the homogeneous nucleation. Similar observations have been noticed by Janneck et al. where a slow shearing speed is used but the solvent and deposition temperature are fixed.[37] Type II thin films show uniform and smooth morphology while Type III appears like no crystal growth on the substrate. The details of these three different morphology types are further verified by Atomic Force Microscope (AFM) as shown in Figure S2. Surface roughness of Type I (Figure S2a) is 4.74 nm while for Type II it is less than 0.25 nm (Figure S2b-d). From the images under the AFM, crystals of Type III morphology (Figure S2e-h) are actually randomly distributed and they are discontinuous. It is important to mention that the three distinct morphologies could appear at the same T by just changing the solvents. At T = 25 °C (Figure 2a-h), Type I appears for low Tb solvent (e.g. DCM, Figure 2a) and switches to Type II when the solvents with moderate Tb such as chloroform, heptane and toluene are used (Figure 2b-d). By further increasing the boiling point of the solvents (e.g. CB, m-xylene, mesitylene and tetralin), no more organic films can be observed under the POM images (Figure 2e-h). Similar trends can also be observed in other temperatures at 40 °C (Figure 2i-p), 60 °C (Figure 2q-v) and 80 °C (Figure 2w-b*). It is worth to point out that the boiling points of different solvents behave like indicators for the crystal growth rate. If the deposition temperature is getting closer to the Tb, the crystal growth rate will increase, and vice versa. Thus, it is expected that d/dt is a function of Tb and T. As the deposited thin film is in the strip form as shown in Figure 3a, [16,38-41] we can modify Equation (1) to,

dmdt=ρoscavteq                                                                                                                         (2)

where teq is the full coverage equivalent thickness. The relationship between teq and tosc is defined as,

teq=tosc× σ2σ1+σ2                                                                                                                     (3)

tosc is the crystal thickness measured directly from the AFM step profile (inset in Figure 3b) while σ1 and σ2 are the summed coverage percentage of the opening and thin film area respectively as indicated in Figure 3b.

Here we will focus on the Type II morphology as it is uniform across the whole deposited film, and it also implies the governing equation is applicable to a certain range of dm/dt. To verify the Equation (2), we firstly investigate the correlation between v and teq under a range of solute concentrations, while Tb and T are fixed to ensure d/dt remains as a constant. The m-xylene with Tb equals to 139 °C and under 60 °C deposition is used for the study. The solute concentrations are ranging from 4 to 10 mg mL-1. The values of teq and typical crystal morphologies under different v between 100 μm s-1 to 500 μm s-1 are shown in Figure S3 and S4, respectively. By using the double logarithm plot of teq against v (Figure 3c), linear slopes with value close to -1 can be observed, which confirms the inverse proportional relationship between teq and v. As teq × v is directly proportional to dm/dt, and dm/dt is equal to c × d/dt, the linearity of teq × v as a function c in Figure 3d can confirm the assumption of considering d/dt is a constant. The evaporation rate of 1.38  10-11 m3 s-1 could be obtained from the slope at a condition of T = 60 °C, Tb = 139 °C and substrate width a = 1.5 cm. It is important to point out that for the Type II organic thin films with teq ranging from 10 to 45 nm (shaded area in Figure 3c), the corresponding mass transfer rate dm/dt obtained by Equation (2) is approximately 6 × 10-11 (c = 4 mg mL-1) to 15 × 10-11 kg s-1 (c = 10 mg mL-1). Deviation significantly from this range would lead to either Type I or Type III morphologies.

The correlation of the d/dt with T and Tb will be further examined in the following. According to the standard derivation based on the Clausius-Clapeyron equation, Gibbs free energy and the Fick’s law, the solvent evaporation flux with the unit mol m-2 s-1 at the meniscus line can be written as,[17,42,43]

J=DPe∆SvapR(1-TbT)δRT                                                                                                                       (4)

where J is the solvent evaporation flux (mol m-2 s-1), D is temperature dependent diffusivity (m2 s-1), P is atmospheric pressure (Pa), Svap is entropy at equilibrium state (J mol-1 K-1), R is universal gas constant (8.314 J mol-1 K-1),  is the distance far away from meniscus line surface where the solvent gas concentration is negligible. The detailed derivation of Equation (4) can be referred to the supporting information and the work by Janneck et al.[17] It is worth to point out that Equation (4) is based on the steady state and 1D approximation while the meniscus line is relatively short comparing with the substrate dimensions. The solvent evaporation rate is proportional to the evaporation flux by,

d∀dt=JAVm                                                                                                                                 (5)

where A is the area of meniscus surface (m2) and Vm is molar volume (m3 mol-1). After derivation (Equation S15), there are two terms related to T, one has the power of n-1 and one exponential term containing latent heat (L). As L in the exponential term is large (for example L = 36.33 kJ mol-1 for m-xylene), the exponential term will be dominating for the whole processing temperature range (303 K-373 K) which we employed for the experiment. By merging the power term of T and other constants together as F, we get mass transfer rate expression in Arrhenius form:

dmdt=ρoscavteq=cd∀dt=Fe- LRT=Fe- ∆SvapTbRT                                                                              (6)

here the pre-factor F lumps not only solvent properties and geometrical factors, but also solute concentration. Similar form of solvent evaporation rate has been achieved by Janneck et al. before.[17] Instead of using this approach to evaluate the optimized shearing velocity, here we focus on correlating the d/dt term with the equivalent thickness, teq, under different shearing velocities. To verify Equation (6) experimentally, we choose three solvents with significant difference in Tb: chloroform (61.2 °C), toluene (110.5 °C) and m-xylene (139 °C). We perform the blade coating deposition under different temperatures. For m-xylene, the solute concentration is at 8 mg mL-1 due to the high boiling point. For the chloroform and toluene, due to the lower boiling points, a concentration of 4 mg mL-1 is employed to avoid the high mass deposition rate and make it comparable with the m-xylene. It is also noteworthy to mention that different concentration would only affect the pre-factor F and will not affect the extraction of L in Equation (6). The measured teq and typical morphologies of these C8-BTBT thin films under different temperatures are shown in Figure S5 and S6. By fixing the shearing speed at 300 m s-1 and multiplying the ρoscav to teq to obtain mass transfer rate dm/dt, we can plot dm/dt against 1/T in a log scale as shown in Figure 4a. The latent heat of evaporation for these three solvents can be obtained by the slopes of the plot. The corresponding values for the chloroform, toluene and m-xylene are 29.62, 33.86 and 36.13 kJ mol-1, respectively. By comparing these latent heat values with the boiling points of these three solvents (Figure 4b), we can obtain a slope value of 84 J mol-1 K-1, which is very close to Svap and also confirm the validity of Equation (6).[44] The measured values of L and the literature values are compared in Table 2. For the Type II flat thin film morphology we are focusing on, Equation (6) can provide useful growth guidelines to correlate the film thickness, shearing speed, deposition temperature, solute concentration and the types of solvents. It is worth to mention that under different processing condition window of the Type II morphology, the d-spacing of the (00l) out-of-plane and (020) in-plane are measured by the X-ray diffraction (XRD) and shown in Figure S7 and S8, respectively. No significant change in the lattice spacing of out-of-plane as well as in-plane can be observed.

To improve the practicability of mass transfer equation, we rearrange Equation (6) into a form similar to the one suggested by Janneck et al., [17]

dmdt=cVmBe- LRT=cVmBe- ∆SvapTbRT                                                                                                (7)

here B is a factor depending on diffusivity constant, temperature power term and geometry. Replotting with respect to Equation (7) (Figure 4c) yields an average B factor of 3.76 × 10-2 mol s-1 and an average △Svap/R value of 10.48 (Trouton’s law).[44]  It is important to point out that the B factor for chloroform is expected to be smaller than toluene and m-xylene because of the larger .

Lastly, the performance of the staggered structure OFETs based on the C8-BTBT active layers with different types of surface morphology is examined. The electrodes are deposited onto the C8-BTBT by direct transfer so that the thermal damage during metal deposition can be eliminated.[45] The Au electrodes are laminated onto the C8-BTBT such that with channels under test are along the (020) direction.[12] OFETs fabricated by the eight different solvents under T = 25 °C, c = 1 mg mL-1 and v = 100 μm s-1 are tested (corresponding to the thin films from Figure 2a-h). The effective carrier mobility (μ), threshold voltage (VTH) and on-off ratio (Ion/Ioff) against the solvent boiling point are displayed in Figure 5a and Figure S9, respectively. The mobility values are obtained from 10 devices. The red dash line indicates the different morphology types of the samples. Type I devices based on DCM show low μ of 0.64 cm2 V-1 s-1 (Figure S10). No drain current (ID) can be detected in Type III devices (Figure S11). On the other hand, an average mobility of 5.88 cm2 V-1 s-1 and a highest value of 7.68 cm2 V-1 s-1 can be achieved by the Type II C8-BTBT layer. It is important to mention that since we are dealing with stripe-like conduction channels, a MATLAB based program is applied for channel width over length (w/lch) correction (Figure S12). The representative transfer and output curves of the devices are shown in Figure 5b-c while mobility histograms for both uncorrected and corrected results are shown in Figure S13. Under such processing parameters (T = 25 °C, c = 1 mg mL-1 and v = 100 μm s-1), three different solvents including chloroform (61.2 °C), heptane (98.4 °C) and toluene (110.5 °C) can achieve the type II organic thin films. Since we are using the transfer method to fabricate the top source-drain electrodes (see experimental section), the flat surface would ensure a conformal contact between the active layers and the electrodes. On the other hand, the Type I samples with high surface roughness would suffer from a poor contact which would also reflect in the carrier mobility. For a comparison, we utilized thermal evaporation to deposit the top contacts onto the Type I thin films and a carrier mobility of 1.19 cm2 V-1 s-1 can be observed (Figure S14). It is also interesting to mention that the deposition can go to the Landau-Levich regime when the shearing speed is further increased. Wan et al. have optimized the deposition conditions for C8-BTBT under this regime. They noticed that at 60oC, large grain size and crack-free active layer can be obtained.[46] By utilizing similar conditions, we obtained a polycrystalline C8-BTBT with a mobility at 2.10 cm2 V- s-1 only (Figure S15).

- Conclusion

In summary, we used blade coating technique to investigate the growth behavior of C8-BTBT under meniscus-guided coating. The particular roles of four processing parameters including shearing speed, solute concentration, deposition temperature and solvent boiling point were examined. It was demonstrated that v shows inverse proportion to teq, governing the thickness of the deposited films. Meanwhile, c determines the amount of molecule per unit volume supplied to meniscus-line region, which reveals a direct linear proportion to dm/dt. Furthermore, by mathematical derivation and experimental results, we verified the correlation between the crystal growth rate and the latent heat of evaporation of the solvents. By varying these processing parameters, three distinct morphology types could be observed and the films with uniform morphology (Rq < 0.25 nm) provide the highest mobility (average 5.88 cm2 V-1 s-1 and maximum 7.68 cm2 V-1 s-1). Our study here can provide valuable information for the mass production and downsizing of organic electronics.

- Experimental Section

Materials: Silicon substrates with 300 nm thermally grown SiO2 were obtained from Namkang Hi-Tech Co.,Ltd. C8-BTBT was bought from Luminescence Technology Corp. Phenyltrichlorosilane (PTS), heptane and tetralin were from J&K Scientific. Dichloromethane, toluene, chlorobenzene, m-xylene were purchased from Sigma-Aldrich. Chloroform and mesitylene were from EMD Millipore Corporation and International Laboratory USA, respectively. All materials were directly used without further purification.

OFET Devices Fabrication: Si/SiO2 substrates were diced into 1.5 cm × 1.5 cm size without further cleaning. Blown with nitrogen gas, the substrates were put into oxygen plasma for hydrophilic treatment (Harrick Scientific, PDC-001, 30 W, 1 h). After that, 100 μL PTS and oxygen plasma treated Si/SiO2 substrates were put into an oven with temperature of 150 °C and a vacuum pressure of 15 torr for 1 h to generate PTS self-assembly-monolayer by vapor phase. Blade coating process for crystal deposition was reported in our previous work.[23] Note that for comparison of crystal morphology by various solvents, moderate v = 100 μm s-1 was used and a consistent c of 1 mg mL-1 was adopted for the limited solubility for alkyl-based heptane. Different parameters were selected for factors investigation with the purpose of falling crystal morphology to Type II including v (c = 4, 6, 8, 10 mg mL-1, Tb = 139 °C and T = 60 °C), c (v = 200 μm s-1, Tb = 139 °C and T = 60 °C), T and Tb (v = 300 μm s-1, c = 8 mg mL-1 for m-xylene and c = 4 mg mL-1 for chloroform and toluene) and electrical studies (v = 100 μm s-1, c = 1 mg mL-1, and T = 25 °C). Detailed parameter determination could be found in main text. After crystal thin films deposition, top source and drain electrodes were fabricated by gold (Au) transfer method. After Si/SiO2 substrate was hydrophobic treated by immersion as reported previously, Au was thermally deposited with TEM copper grid as mask (~ 200 μm × 40 μm in size) to form the Au electrodes.[47] The evaporation rate, thickness and vacuum base pressure were 0.2 Å s-1, 200 nm and 5 × 10-6 Torr, respectively. Au electrodes were transferred from Si/SiO2 substrate to crystal surface by tip with assistance of microscope. Channel width was determined by copper grid mask (200 μm) while the channel length was visually set as ~ 200 μm in Au transferring method to generate an uncorrected w/lch ratio of approximately 1. Accurate w/lch ratio would be measured and corrected using MATLAB program (Figure S12) for following μ extraction. For reference thermally evaporated electrodes, 50 nm Au was deposited at a rate of 0.2 Å s-1 with shadow mask.

Characterization: POM pictures were taken by polarized microscope (Nikon Eclipse LV100N). AFM measurements were carried out by Bruker MultiMode 8 system and NanoScope Analysis software was employed for analysis. The XRD measurements were carried out using Rigaku SmartLab X-Ray diffractometer with a power of 9 kW. Out of plane results were obtained by 2mode. For in-plane test, and 2 scans were used to capture the in-plane signal with an incident X-ray angle of 0.15° and detector moving horizontally. For certain investigated parameter, the other three factors are kept constant. For v investigation, c = 8 mg mL-1, T = 60 °C and Tb = 139 °C; for c investigation, v = 200 m s-1, T = 60 °C and Tb = 139 °C; for T investigation, v = 200 m s-1, c = 8 mg mL-1 and Tb = 139 °C; For Tb investigation, v = 200 m s-1, c = 8 mg mL-1 and T = 60 °C. We used dual source Keithley 2636 to test organic transistors electrical performance including transfer and output curves. Before testing, organic semiconductors were scratched along the edges of electrodes to reduce fringe effect.[48] During transfer curve test, ID was measured as VG swept while keeping VD constant of -80 V. For output measurement, various VG were fixed with VD changing from 0 to -80V. μ were extracted using saturation ID-VG equation:

ID=μCox2wlchVG-VT2                                                                                                            (8)

where Cox is areal capacitance (for 300 nm thermally growth SiO2, Cox = 11 nF cm-2), w and lch are width and length of conduction channel. μ values were averaged from 10 devices for statistical study.

Supporting Information

Supporting Information is available from the Wiley Online Library or from the author.

Acknowledgements

The authors gratefully acknowledge support from the General Research Fund (GRF) under Grant No. HKU 17204517 and HKU 17264016 and the Collaborative Research Fund (CRF) under Grant No. C704514E.

Received: ((will be filled in by the editorial staff))
Revised: ((will be filled in by the editorial staff))
Published online: ((will be filled in by the editorial staff))

References

[1]	K. Pei, X. Ren, Z. Zhou, Z. Zhang, X. Ji, P. K. L. Chan, Adv. Mater. 2018, 30, 1706647.

[2]	B. Peng, S. Huang, Z. Zhou, P. K. L. Chan, Adv. Funct. Mater. 2017, 27, 1700999.

[3]	Z. Wang, S. Guo, H. Li, B. Wang, Y. Sun, Z. Xu, X. Chen, K. Wu, X. Zhang, F. Xing, L. Li, W. Hu, Adv. Mater. 2019, 31, 1805630.

[4]	X. Ren, K. Pei, B. Peng, Z. Zhang, Z. Wang, X. Wang, P. K. L. Chan, Adv. Mater. 2016, 28, 4832.

[5]	A. Yamamura, S. Watanabe, M. Uno, M. Mitani, C. Mitsui, J. Tsurumi, N. Isahaya, Y. Kanaoka, T. Okamoto, J. Takeya, Sci. Adv. 2018, 4, eaao5758.

[6]	U. Zschieschang, M. J. Kang, K. Takimiya, T. Sekitani, T. Someya, T. W. Canzler, A. Werner, J. Blochwitz-Nimoth, H. Klauk, J. Mater. Chem. 2012, 22, 4273.

[7]	Y. Diao, B. C. Tee, G. Giri, J. Xu, D. H. Kim, H. A. Becerril, R. M. Stoltenberg, T. H. Lee, G. Xue, S. C. B. Mannsfeld, Z. Bao, Nat. Mater. 2013, 12, 665.

[8]	Z. Zhang, B. Peng, X. Ji, K. Pei, P. K. L. Chan, Adv. Funct. Mater. 2017, 27, 1703443.

[9]	F. G. del Pozo, S. Fabiano, R. Pfattner, S. Georgakopoulos, S. Galindo, X. Liu, S. Braun, M. Fahlman, J. Veciana, C. Rovira, X. Crispin, M. Berggren, M. Mas-Torrent, Adv. Funct. Mater. 2016, 26, 2379.

[10]	R. Hofmockel, U. Zschieschang, U. Kraft, R. Rödel, N. H. Hansen, M. Stolte, F. Würthner, K. Takimiya, K. Kern, J. Pflaum, H. Klauk, Org. Electron. 2013, 14, 3213.

[11]	G. Giri, E. Verploegen, S. C. B. Mannsfeld, S. Atahan-Evrenk, D. H. Kim, S. Y. Lee, H. A. Becerril, A. Aspuru-Guzik, M. F. Toney, Z. Bao, Nature 2011, 480, 504.

[12]	Z. Zhou, Z. Zhang, Q. Wu, X. Ji, J. Wang, X. Zeng, S. P. Feng, P. K. L. Chan, ACS Appl. Mater. Interfaces 2018, 10, 35395.

[13]	S. Arai, S. Inoue, T. Hamai, R. Kumai, T. Hasegawa, Adv. Mater. 2018, 30, 1707256.

[14]	Y. Li, J. Wan, D-M. Smilgies, N. Bouffard, R. Sun, R. L. Headrick, Sci. Rep. 2016, 6, 32620.

[15]	J. Jang, S. Nam, K. Im, J. Hur, S. N. Cha, J. Kim, H. B. Son, H. Suh, M. A. Loth, J. E. Anthony, J-J. Park, C. E. Park, J. M. Kim, K. Kim, Adv. Funct. Mater. 2012, 22, 1005.

[16]	Z. Chai, S. A. Abbasi, A. Busnaina, ACS Appl. Mater. Interfaces 2018, 10, 18123.

[17]	R. Janneck, F. Vercesi, P. Heremans, J. Genoe, C. Rolin, Adv. Mater. 2016, 28, 8007.

[18]	F. Zhang, E. Mohammadi, X. Luo, J. Strzalka, J. Mei, Y. Diao, Langmuir 2018, 34,1109.

[19]	I. Vladimirov, M. Kellermeier, T. Geßner, Z. Molla, S. Grigorian, U. Pietsch, L. S. Schaffroth, M. Kühn, F. May, R. T. Weitz, Nano Lett. 2018, 18, 9.

[20]	V. K. LaMer, R. H. Dinegar, J. Am. Chem. Soc. 1950, 72, 4847.

[21]	X. Zhao, T. Liu, Y. Cui, X. Hou, Z. Liu, X. Dai, J. Kong, W. Shi, T. J. S. Dennis, Nanoscale 2018, 10, 8170.

[22]	O. Goto, S. Tomiya, Y. Murakami, A. Shinozaki, A. Toda, J. Kasahara, D. Hobara, Adv. Mater. 2012, 24, 1117.

[23]	B. Peng, Z. Wang, P. K. L. Chan, J. Mater. Chem. C 2016, 4, 8628.

[24]	D. He, Y. Zhang, Q. Wu, R. Xu, H. Nan, J. Liu, J. Yao, Z. Wang, S. Yuan, Y. Li, Y. Shi, J. Wang, Z. Ni, L. He, F. Miao, F. Song, H. Xu, K. Watanabe, T. Taniguchi, J. B.   Xu, X. Wang, Nat. Commun. 2014, 5, 5162.

[25]	Q. Wang, J. Qian, Y. Li, Y. Zhang, D. He, S. Jiang, Y. Wang, X. Wang, L. Pan, J. Wang,    X. Wang, Z. Hu, H. Nan, Z. Ni, Y. Zheng, Y. Shi, Adv. Funct. Mater. 2016, 26, 3191.

[26]     H. H. Choi, Y. I. Rodionov, A. F. Paterson, J. Panidi, D. Saranin, N. Kharlamov, S. I.  Didenko, T. D. Anthopoulos, K. Cho, V. Podzorov, Adv. Funct. Mater. 2018, 28, 1707105.

[27]	H. H. Choi, A. F. Paterson, M. A. Fusella, J. Panidi, O. Solomeshch, N. Tessler, M. Heeney, K. Cho, T. D. Anthopoulos, B. P. Rand, V. Podzorov, Adv. Funct. Mater. 2019,    DOI: 10.1002/adfm.201903617.

[28]	E. W. Washburn, International critical tables of numerical data, physics, chemistry and     technology, Knovel, New York, 2003.

[29]	C. L. Yaws, Chemical properties handbook, McGraw-Hill, New York, 1999.

[30]	R. Janneck, P. Heremans, J. Genoe, C. Rolin, Adv. Mater. Interfaces 2018, 5, 1800147.

[31]	M. L. Berre, Y. Chen, D. Baigl, Langmuir 2009, 25, 2554.

[32]	G. Gbabode, M. Dohr, C. Niebel, J.-Y. Balandier, C. Ruzié, P. Négrier, D. Mondieig,   Y. H. Geerts, R. Resel, M. Sferrazza, ACS Appl. Mater. Interfaces 2014, 6, 13413.

[33]	L. Li, P. Gao, W. Wang, K. Müllen, H. Fuchs, L. Chi, Angew. Chem., Int. Ed. 2013, 52, 12530.

[34]	D. Wu, M. Kaplan, H. W. Ro, S. Engmann, D. A. Fischer, D. M. DeLongchamp, L. J. Richter, E. Gann, L. Thomsen, C. R. McNeill, X. Zhang, Chem. Mater. 2018, 30, 1924.

[35]	E. M. Horstman, P. Kafle, F. Zhang, Y. Zhang, P. J. A. Kenis, Y. Diao, ACS Appl. Mater. Interfaces 2018, 10, 10480.

[36]	J. Shin, T. R. Hong, T. W. Lee, A. Kim, Y. H. Kim, M. J. Cho, D. H. Choi, Adv. Mater. 2014, 26, 6031.

[37]	R. Janneck, D. Karagiannis, P. Heremans, J. Genoe, C. Rolin, Adv. Mater. Interfaces   2019, DOI: 10.1002/admi.201900614.

[38]	J. Huang, F. Kim, A. R. Tao, S. Connor, P. Yang, Nat. Mater. 2005, 4, 896.

[39]	T. P. Corrales, M. Bai, V. del Campo, P. Homm, P. Ferrari, A. Diama, C. Wagner, H. Taub, K. Knorr, M. Deutsch, M. J. Retamal, U. G. Volkmann, P. Huber, ACS nano 2014, 8, 9954.

[40]	A. M. Cazabat, F. Heslot, S. M. Troian, P. Carles, Nature 1990, 346, 824.

[41]	R. Janneck, N. Pilet, S. P. Bommanaboyena, B. Watts, P. Heremans, J. Genoe, C. Rolin, Adv. Mater. 2017, 29, 1703864.

[42]	D. Koutsoyiannis, Eur. J. Phys. 2012, 33, 295.

[43]	C. Rolin, S. R. Forrest, Appl. Phys. Lett. 2013, 103, 041911.

[44]	R. M. Digilov, M. Reiner, Eur. J. Phys. 2004, 25, 15.

[45]	Z. Wei, Y. Tong, P. Zhao, X. Zhao, Q. Tang, Y. Liu, Appl. Surf. Sci. 2019, 480, 523.

[46]	J. Wan, Y. Li, J. G. Ulbrandt, D-M. Smilgies, J. Hollin, A. C. Whalley, R. L. Headrick,   APL Mater. 2016, 4, 016103.

[47] 	Z. Zhang, X. Ren, B. Peng, Z. Wang, X. Wang, K. Pei, B. Shan, Q. Miao, P. K. L. Chan,   Adv. Funct. Mater. 2015, 25, 61.

[48]	K. Pei, M. Chen, Z. Zhou, H. Li, P. K. L. Chan, ACS Appl. Electron. Mater. 2019, 1, 379.

Figure 1. Schematic illustration of blade coating setup. a) Overview diagram of the setup. C8-BTBT solution is sandwiched by hydrophobic blade and growing substrate whose temperature could be controlled to assist solvent evaporation. As the substrate moves forward driven by moving stage, thin films of semiconductor would deposit on the substrate gradually. b) Magnification view of thin film deposition process in which a and tosc represent the width and thickness of thin film while c stands for the solute concentration.

Figure 2. Qualitive study of the effect of Tb and T on organic semiconductor POM morphology. Inset coordinate indicates Tb and T increase sequence. Eight columns corresponds to solvents with different Tb: a,i) dichloromethane, b,j) chloroform, c,k,q,w) heptane, d,l,r,x) toluene, e,m,s,y) chlorobenzene, f,n,t,z) m-xylene, g,o,u,a*) mesitylene, and h,p,v,b*) tetralin. Horizontally, organic thin films are deposited at various deposition temperatures: a-h) 25 °C, i-p) 40 °C, q-v) 60 °C and w-b*) 80 °C from top row to bottom one. Scale bar is shown in (b*) while white arrow in (b*) points out the solution shearing direction.

Figure 3. v and c effect on crystal growth rate. a) Typical AFM image of stripe shape crystal morphology. b) Histogram percentage of height distribution of (a) while inset depicts the cross-section profile along the white dash line in (a) for tosc measurement. Two peaks σ1 and σ2 represent sum of histogram percentage of lower and higher regions in (a), respectively. c) Double logarithm of teq-v relationships for various c ranging from 4 to 10 mg mL-1 with a step of 2 mg mL-1. Fitting slopes are labelled for each c to verify the inverse proportional relationship between teq and v. d) Linear relationship plot for teq × v and dm/dt with respect to c. teq used for computation is extracted at v = 200 μm s-1 as indicated by black arrow in (c).

Figure 4. Effect of T and Tb on crystal growth rate and practicability for growth rate prediction. a) Logarithm plot of dm/dt versus 1/T for latent heat energy extraction. Three solvents with various Tb are used here: chloroform (61.2 °C), toluene (110.5 °C) and m-xylene (139 °C). b) Plot of experimental L extracted from slopes in (a) with respect to Tb. A slope of 84 J mol-1 K-1 could be obtained, which is closer to △Svap. This result illustrates energy barrier during blade coating is equal the latent heat of solvents (L = Tb × △Svap). c) Replot of predictivity of mass transfer rate equation. An average B of 3.76 × 10-2 mol s-1 and a △Svap/R of 10.48 are extracted from the fitting. The B factors for chloroform, toluene and m-xylene are 1.3 × 10-2 mol s-1, 4.4 × 10-2 mol s-1, 5.57 × 10-2 mol s-1, respectively.

Figure 5. Electrical characterization of organic semiconductor thin films. a) Statistical μ (from 10 OFET devices) with respect to different Tb by using different solvents. Red lines separate types of thin films. Higher mobility could be achieved in Type II thin films with an average value of 5.88 cm2 V-1 s-1, compared with Type I thin films with average mobility of 0.64 cm2 V-1 s-1. b-c) Representative transfer and output curves of device fabricated form Type II crystal deposited from chloroform. In (b), black curve and red curve stand for ID and ID0.5 respectively while blue curve indicates gate leakage current (IG). Output curve in (c) is tested at a VG step of -20 V.

Table 1. Solvent properties of boiling point (Tb) and surface tension (γ*) (at 25 °C).

| Solvent | Tb [°C][28] | γ* [mN m-1][29] |
| --- | --- | --- |
| Dichloromethane | 40.1 | 28.77 |
| Chloroform | 61.2 | 26.68 |
| Heptane | 98.4 | 19.78 |
| Toluene | 110.5 | 27.93 |
| Chlorobenzene | 132.1 | 32.93 |
| M-xylene | 139 | 28.26 |
| Mesitylene | 164.6 | 28.05 |
| Tetralin | 207.2 | 33.16 |

Table 2. Boiling point (Tb), Experimental latent heat (L), L in literature and entropy at equilibrium (△Svap) for various solvents.

| Solvent | Chloroform | Toluene | M-xylene |
| --- | --- | --- | --- |
| Tb [K][28] | 334.2 | 383.5 | 412 |
| Experimental L [kJ mol-1] | 29.62 | 33.86 | 36.13 |
| L in literature [kJ mol-1][29] | 29.79 | 33.59 | 36.33 |
| △Svap = L/Tb | 89.14 | 87.59 | 88.18 |

The table of contents

Elementary factors involved in meniscus-guided coating are systematically studied to identify their roles during the semiconductor thin film deposition process. Mathematical equations are derived to unify the influence of shearing speed, solute concentration, deposition temperature and solvent boiling point. The effect is further verified experimentally, which gives deep insight into thin film growth modulation.

Keyword: crystal growth, blade coating, semiconductor morphology, organic transistors

M. Chen, B. Peng, S. Huang, P. K. L. Chan*

Title: Understanding the Meniscus-Guided Coating Parameters in Organic Field-Effect-Transistor Fabrications

ToC figure (55 mm broad × 50 mm high)